## Slide 1
Lifted electrodes on a SiO₂ buffer:
removing the lift-position standing wave
femwell / scikit-fem eigenmode study at λ = 1575 nm
Notes: Lisbon lifted electrodes show an insertion loss that oscillates with the lift position. We show where it comes from, how a 200 nm SiO2 buffer removes it, what it costs in Vpi*L, and the final buffer/gap choice.

## Slide 2
Lifting the gold: same Vπ·L, but IL oscillates with x_lift
Cordoba (gold flat on the LN slab) vs Lisbon (gold lifted onto SiO₂ at x_lift), both with a 4.2 µm gap
Cordoba (legacy)
Lisbon (lifted)
2.260 | 2.265
Vπ·L [V·cm], Cordoba | Lisbon
identical (Δ 0.2 %)
x_lift
distance from the rib centre
to the gold/oxide step
Chart: Insertion loss vs lift position
| 6.5 | 6.6 | 6.7 | 6.8 | 6.9 | 7.0 | 7.1 | 7.2 | 7.3 | 7.4 | 7.5 | 7.6 | 7.7 | 7.8 | 7.9 | 8.0 | 8.1 | 8.2 | 8.3 | 8.4 | 8.5 | 8.6 | 8.7 | 8.8 | 8.9 | 9.0 | 9.1 | 9.2 | 9.3 | 9.4 | 9.5 | 9.6 | 9.7 | 9.8 | 9.9 | 10.0 | 10.1 | 10.2 | 10.3 | 10.4 | 10.5 | 10.6 | 10.7 | 10.8 | 10.9 | 11.0 | 12.1
Lisbon, lifted | 0.6815 | 0.3521 | 0.2271 | 0.1826 | 0.1807 | 0.2216 | 0.3345 | 0.6016 | 0.8827 | 0.6382 | 0.3731 | 0.2513 | 0.2077 | 0.2073 | 0.2509 | 0.3633 | 0.5965 | 0.7824 | 0.6002 | 0.3825 | 0.2751 | 0.231 | 0.2329 | 0.2782 | 0.391 | 0.585 | 0.7076 | 0.566 | 0.3916 | 0.2914 | 0.2525 | 0.2549 | 0.3051 | 0.4036 | 0.5742 | 0.6495 | 0.5403 | 0.3937 | 0.3071 | 0.2723 | 0.276 | 0.3228 | 0.4169 | 0.5605 | 0.6071 | 0.5169 | 0.3284
Cordoba, legacy (0.42 dB/cm) | 0.4202 | 0.4202
x_lift 7.1 → 7.2 µm | 0.3345 | 0.6016
+80 %
IL for a 100 nm shift of x_lift
(0.33 → 0.60 dB/cm)
0.18 – 0.88
IL range [dB/cm] within
0.4 µm of x_lift (period 0.9 µm)
Notes: Geometries drawn from the model polygons, same scale. x_lift = distance from the rib centre to the point where the gold leaves the LN slab and climbs onto the SiO2 lift. Vpi*L: Cordoba 2.260, Lisbon 2.265 V*cm at the same 4.2 um gap. IL of Lisbon oscillates between 0.18 and 0.88 dB/cm with a 0.9 um period around the Cordoba value 0.42 dB/cm. Red points: 7.1 -> 7.2 um, the steepest 100 nm step (0.33 -> 0.60 dB/cm). Lithography/overlay errors of this size are realistic, so the IL of a fabricated device is not predictable. Data: results/lift_sweep.csv.

## Slide 3
Origin: a standing wave under the gold
|E|² along the slab: ripples appear under the gold in the lifted design, not in the legacy one
Gold on the LN slab guides a surface wave
n = 2.07 > n_rib = 1.88
The rib mode leaks into it; the wave travels sideways
and is reflected at the gold/oxide step
Standing wave: period 0.9 µm
IL peaks when x_lift makes the cavity resonant
Cordoba: no step, so the wave simply travels away and is absorbed: smooth curve, no x_lift dependence.
Notes: Left: |E|^2 at slab mid-height vs x. Dip (x_lift 6.9 um, IL 0.18) and peak (7.3 um, IL 0.88) show ripples between the gap edge and the lift; legacy (no lift) shows a smooth, slowly decaying travelling wave. Right: field maps, same dB scale. The gold/LN interface supports a lossy surface wave with index about 2.07, above the rib mode index 1.884, so it is phase-matched to leak sideways. The step where the gold leaves the slab reflects it; the reflected wave interferes with the incoming one. Ripple period 0.90 um = pi/k_x predicted by a 1D model (0.91 um).

## Slide 4
SiO₂ buffer: the standing wave can no longer form
200 nm SiO₂ under the whole electrode and across the gap; bottom gap 4.2 → 3.2 µm
Lisbon on a SiO₂ buffer
Chart: Index of the wave under the gold
| 0.0 | 5.0 | 10.0 | 15.0 | 20.0 | 25.0 | 30.0 | 35.0 | 40.0 | 45.0 | 50.0 | 75.0 | 100.0 | 125.0 | 150.0 | 175.0 | 200.0 | 225.0 | 250.0 | 275.0 | 300.0
wave under the gold | 2.0722 | 2.0336 | 2.0013 | 1.9737 | 1.9497 | 1.9287 | 1.91 | 1.8932 | 1.8781 | 1.8643 | 1.8517 | 1.8019 | 1.7665 | 1.7398 | 1.719 | 1.7022 | 1.6884 | 1.6769 | 1.6672 | 1.659 | 1.6519
rib mode | 1.8838 | 1.8838
cutoff ≈ 38 nm | 1.62 | 2.1
design | 1.6884
Chart: Insertion loss vs lift position
Lisbon, no buffer, gap 4.2 µm | 0.6815 | 0.3521 | 0.2271 | 0.1826 | 0.1807 | 0.2216 | 0.3345 | 0.6016 | 0.8827 | 0.6382 | 0.3731 | 0.2513 | 0.2077 | 0.2073 | 0.2509 | 0.3633 | 0.5965 | 0.7824 | 0.6002 | 0.3825 | 0.2751 | 0.231 | 0.2329 | 0.2782 | 0.391 | 0.585 | 0.7076 | 0.566 | 0.3916 | 0.2914 | 0.2525 | 0.2549 | 0.3051 | 0.4036 | 0.5742 | 0.6495 | 0.5403 | 0.3937 | 0.3071 | 0.2723 | 0.276 | 0.3228 | 0.4169 | 0.5605 | 0.6071 | 0.5169 | 0.3284
Above 38 nm the wave under the gold falls below the rib index: it is cut off.
At 200 nm it decays by 29 dB/µm: nothing reaches the step, nothing is reflected.
Result: IL = 0.048 dB/cm, flat (±0.1 %) for x_lift 3.8–30 µm.
Check: the 1D cutoff model reproduces the 2D ripple periods and decay rates within about 5 %.
Notes: Chart top right: 1D effective index of the wave guided under the gold vs buffer thickness (mean of the two in-plane LN permittivities; cutoff 37-39 nm). Below the rib index the wave cannot be phase matched, so the rib mode cannot couple into a propagating wave: there is no standing wave to form, whatever x_lift. The 1D model matches the 2D simulations (period 0.90 vs 0.91 um at 0 nm; decay 28.98 vs 28.95 dB/um at 200 nm). Bottom: 200 nm buffer, 88 lift positions 3.8-30.1 um, IL 0.0480-0.0481 dB/cm. Chart shows up to 12.6 um; flat also at 16-30 um. Without buffer at gap 3.2 IL would be 4-30 dB/cm and still oscillating.

## Slide 5
The price: higher Vπ·L, recovered with a narrower gap
The DC field must cross the low-ε oxide (ε 3.75 vs 28 in LN); narrowing the gap compensates
Chart: Vπ·L vs buffer (gap 3.2 µm)
| 0 | 25 | 50 | 100 | 150 | 200 | 250 | 300
Vπ·L | 1.6496 | 1.7989 | 1.8784 | 1.9912 | 2.0767 | 2.1484 | 2.212 | 2.2703
200 nm | 2.1484
Chart: Vπ·L vs gap (200 nm buffer)
| 2.4 | 2.6 | 2.8 | 3.0 | 3.2 | 3.4 | 3.6
Vπ·L | 1.6353 | 1.7704 | 1.8993 | 2.0249 | 2.1484 | 2.2707 | 2.392
3.4 µm | 2.2707
Chart: IL vs gap (200 nm buffer)
| 2.4 | 2.6 | 2.8 | 3.0 | 3.2 | 3.4 | 3.6
IL | 0.6509 | 0.3257 | 0.1689 | 0.0895 | 0.0481 | 0.026 | 0.0142
3.4 µm | 0.026
Trade-off: at a fixed gap the buffer raises Vπ·L by 30 % (1.65 → 2.15 V·cm at 3.2 µm).
Buffer 200 nm: 5× the 38 nm cutoff, safe against thickness errors. 150 nm would cut Vπ·L by only 3 % and raise IL by 41 %.
Gap 3.4 µm: Vπ·L 2.27 V·cm, the same as the original 4.2 µm design (2.26), with IL 0.026 dB/cm and no x_lift dependence.
Final design: buffer 200 nm, gap 3.4 µm
2.27
Vπ·L [V·cm]
0.026
IL [dB/cm], flat
1.65 V
Vπ on the line (< 1.7 V)
Vπ = Vπ·L / (L × duty) = 2.27 / (1.484 cm × 0.925) = 1.65 V
line L = 14.84 mm, duty cycle 0.925
Notes: Left: Vpi*L vs buffer thickness at gap 3.2 um, x_lift 7 um (150, 250 nm added for this deck). 150 nm: Vpi*L 2.077 vs 2.148 V*cm (-3.3 %), IL 0.068 vs 0.048 dB/cm. Centre/right: gap scan at 200 nm (GAP_TOP fixed at 10 um). Vpi*L grows linearly with the gap, IL falls exponentially. Gap 3.4 um: Vpi*L 2.2707 V*cm, IL 0.0260 dB/cm, flat for x_lift 4.5-16 um (2.270-2.275 V*cm). On the 14.84 mm line with duty cycle 0.925: Vpi = 1.654 V. The 1.7 V limit allows Vpi*L up to 2.334 V*cm (gap about 3.5 um), so 3.4 um keeps about 0.05 V of margin. Gold loss over the line: 0.039 dB.