## Slide 1
Buffered design: robust to buffer-thickness error
SiO₂ buffer 130 → 270 nm (10 nm step), gap 3.4 µm, CAP 2.0 × 1.4 µm; measured spread ±20 nm (±40 nm extreme)
rib top WG_TOP = 1.0 µm
Chart: Vπ·L (V·cm)
| 130.0 | 140.0 | 150.0 | 160.0 | 170.0 | 180.0 | 190.0 | 200.0 | 210.0 | 220.0 | 230.0 | 240.0 | 250.0 | 260.0 | 270.0
Lisbon, C band 1575 nm | 2.1696 | 2.1859 | 2.2016 | 2.2167 | 2.2313 | 2.2455 | 2.2593 | 2.2727 | 2.2859 | 2.2987 | 2.3113 | 2.3235 | 2.3356 | 2.3474 | 2.359
Jerez, O band 1360 nm | 1.804 | 1.8163 | 1.8282 | 1.8396 | 1.8507 | 1.8615 | 1.8719 | 1.8821 | 1.892 | 1.9017 | 1.9112 | 1.9205 | 1.9297 | 1.9387 | 1.9474
_refL | 2.2668 | 2.2668
_refJ | 1.9154 | 1.9154
_w160 | 1.65 | 2.45
_w180 | 1.65 | 2.45
_w220 | 1.65 | 2.45
_w240 | 1.65 | 2.45
_n200 | 1.65 | 2.45
Chart: SiO₂ buffer thickness (nm)
| 130.0 | 140.0 | 150.0 | 160.0 | 170.0 | 180.0 | 190.0 | 200.0 | 210.0 | 220.0 | 230.0 | 240.0 | 250.0 | 260.0 | 270.0
Lisbon, C band 1575 nm | 0.043508 | 0.040441 | 0.037686 | 0.035188 | 0.032876 | 0.030747 | 0.028745 | 0.026878 | 0.02512 | 0.023493 | 0.021955 | 0.020512 | 0.019144 | 0.017855 | 0.016648
Jerez, O band 1360 nm | 0.026588 | 0.024408 | 0.022482 | 0.020753 | 0.019169 | 0.017736 | 0.016389 | 0.015151 | 0.013997 | 0.01293 | 0.011942 | 0.011022 | 0.010164 | 0.00936 | 0.0086164
_w160 | 0.005 | 0.1
_w180 | 0.005 | 0.1
_w220 | 0.005 | 0.1
_w240 | 0.005 | 0.1
_n200 | 0.005 | 0.1
rib top WG_TOP = 1.4 µm
Chart: Vπ·L (V·cm)
| 130.0 | 140.0 | 150.0 | 160.0 | 170.0 | 180.0 | 190.0 | 200.0 | 210.0 | 220.0 | 230.0 | 240.0 | 250.0 | 260.0 | 270.0
Lisbon, C band 1575 nm | 2.0748 | 2.0906 | 2.1058 | 2.1205 | 2.1347 | 2.1484 | 2.1617 | 2.1747 | 2.1874 | 2.1998 | 2.2119 | 2.2237 | 2.2353 | 2.2467 | 2.2578
Jerez, O band 1360 nm | 1.7304 | 1.7424 | 1.754 | 1.7651 | 1.7759 | 1.7863 | 1.7964 | 1.8062 | 1.8159 | 1.8254 | 1.8346 | 1.8437 | 1.8525 | 1.8612 | 1.8698
_refL | 2.1734 | 2.1734
_refJ | 1.8405 | 1.8405
_w160 | 1.65 | 2.45
_w180 | 1.65 | 2.45
_w220 | 1.65 | 2.45
_w240 | 1.65 | 2.45
_n200 | 1.65 | 2.45
Chart: SiO₂ buffer thickness (nm)
| 130.0 | 140.0 | 150.0 | 160.0 | 170.0 | 180.0 | 190.0 | 200.0 | 210.0 | 220.0 | 230.0 | 240.0 | 250.0 | 260.0 | 270.0
Lisbon, C band 1575 nm | 0.045656 | 0.042624 | 0.039845 | 0.037309 | 0.034935 | 0.032738 | 0.030662 | 0.028717 | 0.026881 | 0.025174 | 0.02356 | 0.022042 | 0.020601 | 0.019241 | 0.017967
Jerez, O band 1360 nm | 0.028422 | 0.026166 | 0.024143 | 0.022308 | 0.020622 | 0.019084 | 0.017639 | 0.016304 | 0.015064 | 0.013921 | 0.012861 | 0.011872 | 0.010949 | 0.010084 | 0.0092878
_w160 | 0.005 | 0.1
_w180 | 0.005 | 0.1
_w220 | 0.005 | 0.1
_w240 | 0.005 | 0.1
_n200 | 0.005 | 0.1
━● Lisbon, C band 1575 nm ━● Jerez, O band 1360 nm dashed horizontal: unbuffered at gap 4.2 µm; verticals: 200 nm nominal (navy), ±20 nm (grey solid), ±40 nm (grey dashed)
Notes: Buffered lifted designs, gap 3.4 um, GAP_TOP 10 um, CAP_W 2.0 um, CAP_H 1.4 um from the buffer top (the cap moves with the buffer), 60 deg sidewalls. Lisbon: 550 nm film, 275 nm etch / 275 nm slab, 1575 nm. Jerez: 400 nm film, 170 nm etch / 230 nm slab, 1360 nm. Sellmeier LN (Zelmon) and SiO2 (Malitson), Johnson & Christy gold, converged mesh. Buffer 130-270 nm in 10 nm steps (60 runs) plus the unbuffered references at gap 4.2 um (dashed). Vpi*L is linear in the buffer thickness (deviation <= 6 mV*cm over the range): +1.3 mV*cm/nm (Lisbon) and +1.0 mV*cm/nm (Jerez), i.e. about +/-1.1 % at +/-20 nm and +/-2.3 % at +/-40 nm, the same for both rib widths. IL falls exponentially with the buffer (e-folding 150 nm Lisbon, 125 nm Jerez): about +/-15 % at +/-20 nm, but always below 0.036 dB/cm inside the +/-40 nm window. No ripple and no x_lift dependence appears anywhere in the range: the lateral wave under the gold stays cut off.

## Slide 2
Measured buffer spread → Vπ·L and IL spread
Process data (32 chips per wafer) mapped onto the simulated sweep; rib top 1.0 µm
wafer | buffer (nm) | Lisbon Vπ·L (V·cm) | Lisbon IL (dB/cm) | Jerez Vπ·L (V·cm) | Jerez IL (dB/cm)
sil-A | 194 ± 18 (167–231) | 2.265 ± 0.025 | 0.028 (0.022–0.034) | 1.876 ± 0.019 | 0.016 (0.012–0.020)
sil-B | 214 ± 16 (189–246) | 2.291 ± 0.021 | 0.025 (0.020–0.029) | 1.896 ± 0.016 | 0.014 (0.010–0.017)
sil-C | 248 ± 16 (226–279) | 2.334 ± 0.018 | 0.019 (0.016–0.023) | 1.928 ± 0.014 | 0.010 (0.008–0.012)
no buffer, gap 4.2 | — | 2.267 | 0.23 (on ripple) | 1.915 | 0.075 (on ripple)
±1.1 %
Vπ·L per ±20 nm
(±2.3 % at ±40 nm)
±0.025
V·cm: Vπ·L chip-to-chip σ
(sil-A, Lisbon)
≤ 0.036
dB/cm IL, any chip
(buffer ≫ 38 nm cutoff)
235 nm
Jerez: buffer up to which gap 3.4
beats the unbuffered gap 4.2
Robust: the process spread moves Vπ·L by about 1 % and keeps IL ≤ 0.036 dB/cm; the wave under the gold stays cut off on every chip.
Margin: Jerez at gap 3.4 µm beats its unbuffered reference up to a 235 nm buffer; Lisbon matches it at 196 nm, so thicker wafers (sil-B/C) give Vπ·L 1–3 % above it: target the sil-A recipe, or narrow the gap by ≈ 0.1 µm (to be verified).
Notes: Measured 'thick slab post etch' (the 200 nm buffer after etch-back of the ~1.4 um deposition): sil-A 0.194 +/- 0.018, sil-B 0.2135 +/- 0.016, sil-C 0.248 +/- 0.016 um (min-max 167-231, 189-246, 226-279 nm). Each wafer's mean and sigma are mapped through a quadratic fit of the simulated Vpi*L(buffer) and log IL(buffer), rib top 1.0 um (1.4 um behaves the same: Lisbon 2.167 / 2.192 / 2.233, Jerez 1.800 / 1.819 / 1.851 V*cm). IL ranges are for the thinnest/thickest chip; sil-C's thickest chip (279 nm) is a 9 nm extrapolation. Vpi*L sensitivity: +1.34 (Lisbon) / +1.02 (Jerez) mV*cm per nm. Chip-to-chip sigma of Vpi*L on sil-A: 0.025 V*cm (Lisbon), 0.019 V*cm (Jerez). Against the unbuffered gap-4.2 design: Jerez crosses at 235 nm, Lisbon at 196 nm (WG 1.0) / 199 nm (WG 1.4). Narrowing the gap by 0.1 um should recover about 0.06 V*cm for Lisbon (slope ~0.6 V*cm/um from the earlier 150 nm runs at gap 3.2/3.4) - to be checked with a simulation if pursued. Caveat: the model keeps the cap height constant above the buffer; if the cap top is set by the deposition, Vpi*L shifts by about -0.4 %.