## Slide 1
Arm imbalances in a push-pull TW-MZM
Effect on EO bandwidth and eye diagram, and how each is represented in Lumerical INTERCONNECT

## Slide 2
Overview
0
Framework
How the EO bandwidth and the eye are computed
The eye features and how they are measured
The INTERCONNECT schematic, block by block
The two-arm model every imbalance enters
1
The six imbalances
Eye diagrams computed by the code, per value
Equations linking the imbalance to the eye / EO BW
Range, typical value, physical and fabrication cause
2
INTERCONNECT representation
Which block or property carries each imbalance
Summary matrix
Reference device for every number and plot in this deck
Measured line “Jerez” (Touchstone, Lmeas = 2.5 mm) scaled to L = 16.5 mm · RS = 50 Ω, RT = 53 Ω · ng = 2.27 · Vπ = 4 V per arm (2 V push-pull) · 1550 nm, 13 dBm laser (19.95 mW), responsivity 1 A/W
100 Gb/s NRZ, PRBS-9, 2.0 Vpp drive, driver 70 GHz / receiver 75 GHz (4th-order Bessel), 32 samples per bit, receiver noise OFF (so every change seen is caused by the imbalance). Balanced EO BW = 84.47 GHz.

## Slide 3
0.1 How the EO bandwidth is computed
Travelling-wave transfer function of one electrode, then the two-arm combination
Electrode transfer function (per arm, ng of that arm)
Whole modulator, normalisation, bandwidth
α(f), nm(f), Zc(f): fitted to the de-embedded Touchstone, then scaled to L
Plateau window flo..fhi averages the low-frequency ripple; INTERCONNECT’s read-back uses the same window
The prefactor before the bracket is frequency-flat: it cancels on normalisation
Right: normalised EO S21 (top) and electrical S11 (bottom) of the balanced reference device; BW = 84.47 GHz.

## Slide 4
0.2 How the eye diagram is computed
Time-domain simulation of the same device, folded on two unit intervals (UI = 1 / bit rate = 10 ps)
PRBS-9
511-bit pattern,
100 Gb/s
NRZ driver
±Vpp/2 = ±1 V
Bessel-4, 70 GHz
Electrode
H1(f), H2(f)
one per arm
Arm phases
mi = gi(hi ∗ v)
gi = ±π/Vπ,i
Interferometer
Y branch → arms →
Y branch, bias 90°
Photodiode + Rx
1 A/W, Bessel-4,
75 GHz, noise off
Fold + measure
2-UI traces, labelled
by transmitted bit
Output power: two-beam interference of the arm fields
Symbols
a1, a2: arm field amplitudes after the input Y branch · Δφ0: static phase (bias + error) · TY: power transmission of one Y branch · hi: impulse response of Hi
Why it agrees with the EO BW
The eye uses the same electrode function Hi(f) as the bandwidth, evaluated on the FFT grid. The whole PRBS period is one FFT period, so filtering is exact (no edge effects). Delay is removed by cross-correlation.

## Slide 5
0.3 The eye features and how they are measured
The four features
Extinction ratio (aperture)
Height (vertical margin)
Width (timing margin): fraction of UI where worst 1 > worst 0
Rail thickness (cleanness)
Also reported
How they are set: μ and σ are taken at the sampling instant of maximum opening; every trace is labelled by the bit that was sent (no threshold).
Standard instruments (IEEE 802.3) average over the central ~20 % of the UI; identical for flat rails.
Notes: OMA: optical modulation amplitude. X: crossing percentage. Q: quality factor. mu/sigma: mean and standard deviation of the photocurrent of each level at the sampling instant. Dashed lines on the code plots: static maximum/minimum of the transfer curve (infinite bandwidth); dotted: all laser light reaching the detector.

## Slide 6
0.4 The MZM schematic in INTERCONNECT
Built by the API (eye mode). For the EO bandwidth, PRBS/NRZ/EYE are replaced by a network analyser (ENA)
Reading the schematic
Green: optical path
CWL → SPLT_1 → OM_1 / OM_2 (+PHS_1) → SPLT_2 → PIN
Blue: electrical path
PRBS → NRZ → TW_1 / TW_2 → OM modulation ports
Dashed: timing reference
NRZ output → EYE reference (without it no eye is computed)
Why not the built-in MZM element?
It is lumped (π dc/rf voltage, ER, insertion loss): no travelling-wave electrode, so no measured α(f), nm(f), Zc(f).

## Slide 7
0.5 Blocks and the parameters that matter here
Block | INTERCONNECT element | Function | Relevant parameters (reference value)
CWL_1 | CW Laser | Optical carrier | power 13 dBm · frequency 193.414 THz (1550 nm) · linewidth 0
SPLT_1 | Waveguide Y Branch | Input splitter | coupling coefficient 0.5 (→ split error) · insertion loss (→ Y loss)
TW_1, TW_2 | Traveling Wave Electrode | Microwave line, one per arm | length 16.5 mm · optical index ng per arm · loss / Zc / nm tables · RS 50 Ω, RT 53 Ω
OM_1, OM_2 | Optical Modulator Measured | Phase modulation of each arm | input parameter = coefficients · phase coefficient c = ∓π/(Vπ,i·L) · length L = 1 µm · lumped
PHS_1 | Optical Phase Shift | Bias of the interferometer | phase shift = 90° + static phase error (1.5708 rad at quadrature)
ATT_1 | Optical Attenuator | Extra loss in arm 2 (only if ≠ 0) | attenuation = arm loss imbalance (dB)
SPLT_2 | Waveguide Y Branch | Output combiner | coupling coefficient 0.5 · insertion loss (→ Y loss)
PIN_1 | PIN Photodetector | Optical → electrical | responsivity 1 A/W · noise sources off
PRBS_1 / NRZ_1 | PRBS / NRZ Pulse Generator | Drive signal | bitrate 100 Gb/s · order 9 · amplitude 2 · bias −1 (→ ±1 V) · rise/fall period
EYE_1 | Eye Diagram | Eye and its measurements | bitrate 100 Gb/s · input ← PIN · reference ← NRZ · calculate measurements
ENA_1 | Network Analyzer | EO bandwidth mode only | sweep to fmax · output → TW inputs · input ← PIN → normalised S21

## Slide 8
The two-arm model: where each imbalance enters
One equation, six knobs. Only ng changes the frequency dependence, so only it can move the EO bandwidth
1 Arm loss imbalance
changes: amplitude of arm 2
2 Splitter imbalance
changes: both amplitudes
3 Static phase error
changes: operating point
4 Vπ imbalance
changes: modulation efficiency
5 ng imbalance
changes: frequency response
6 Y-branch excess loss
changes: common-mode scale

## Slide 9
1 Arm loss imbalance: effect on the eye
The '0' rail lifts off zero and the top drops: extinction ratio falls; timing is untouched
ΔL (dB) | ER static | ER eye | 1/ER rule | μ1 (mA) | μ0 (mA) | Height (mA) | Mean P (mW) | EO BW (GHz)
0 | ∞ | 17.86 | 17.86 | 19.63 | 0.321 | 17.71 | 10.00 | 84.47
0.3 | 35.26 | 17.79 | 17.78 | 18.97 | 0.316 | 17.11 | 9.66 | 84.47
1 | 24.81 | 17.06 | 17.06 | 17.55 | 0.345 | 15.79 | 8.97 | 84.47
3 | 15.34 | 13.41 | 13.41 | 14.32 | 0.653 | 12.54 | 7.50 | 84.47
Reading it
ER falls: 17.86 → 13.41 dB at 3 dB
Width 0.969 UI and crossing 50 % unchanged
Rails get thinner: the swing is smaller, so is the ISI
“1/ER rule” column: predicted eye ER, matches the code to 0.01 dB
Eyes computed by mzm_interconnect.eye on the reference device. Dashed: static max/min of the transfer curve (infinite bandwidth); dotted: all laser light; vertical dotted: sampling instant.

## Slide 10
1 Arm loss imbalance: mechanism
How it enters the equations
Eye ER = static ceiling combined with the balanced eye's ISI floor (ER_ISI = 17.86 dB):
Range
0 – 3 dB in the GUI. Typical 0 – 0.3 dB: 5 % loss-coefficient difference at 0.2 dB/cm over 16.5 mm is only 0.017 dB; above ~1 dB suspect a localised defect.
Physical / fabrication cause
Different propagation loss in the two arms: sidewall-roughness scattering after an asymmetric over-etch, a mode pushed closer to the metal (absorption), a particle or local defect, unequal bends.
In INTERCONNECT
Optical Attenuator ATT_1 in arm 2, property attenuation = ΔL (dB). Alternative: OM_2 absorption coefficient a. A negative value is modelled by swapping the arms.
EO bandwidth
Unchanged (84.47 GHz at every value): a1a2 is a flat factor.

## Slide 11
2 Splitter imbalance: effect on the eye
Same signature as arm loss, but the mean power stays constant: light is redistributed, not lost
ε (split) | ER static | ER eye | 1/ER rule | μ1 (mA) | μ0 (mA) | Height (mA) | Mean P (mW) | EO BW (GHz)
0 | ∞ | 17.86 | 17.86 | 19.63 | 0.321 | 17.71 | 10.00 | 84.47
0.02 | 33.98 | 17.76 | 17.76 | 19.62 | 0.329 | 17.70 | 10.00 | 84.47
0.1 | 19.91 | 15.76 | 15.76 | 19.44 | 0.516 | 17.36 | 10.00 | 84.47
0.3 | 9.54 | 8.95 | 8.95 | 17.70 | 2.252 | 14.17 | 9.99 | 84.47
Reading it
ER falls smoothly: 17.86 → 15.76 → 8.95 dB
Mean power fixed at 10.0 mW
Width and crossing unchanged
No threshold: at ε = 0.5 all light is in one arm and the interferometer is gone
Eyes computed by mzm_interconnect.eye on the reference device. Dashed: static max/min of the transfer curve (infinite bandwidth); dotted: all laser light; vertical dotted: sampling instant.

## Slide 12
2 Splitter imbalance: mechanism
How it enters the equations
ε = 0.02 → ER_static ≈ 34 dB; ε = 0.1 → 19.9 dB; ε = 0.3 → 9.5 dB
Range
0 – 0.45 in the GUI (deviation of the power fraction from 0.5). Typical 0.005 – 0.02 (50.5:49.5 to 52:48) for a good Y branch or MMI.
Physical / fabrication cause
Geometric asymmetry at the junction: unequal branch widths (lithography / etch bias), unequal branch angles, tip rounding offset, asymmetric over-etch.
In INTERCONNECT
Waveguide Y Branch SPLT_1, coupling coefficient = 1 − ρ = 0.5 − ε (power to port 3 / arm 2). SPLT_2 stays 0.5. No extra block.
EO bandwidth
Unchanged (84.47 GHz): a1a2 is a flat factor.

## Slide 13
3 Static phase error: effect on the eye
The operating point leaves quadrature: rails become asymmetric, the crossing drops, the eye closes past ~60°
φ (deg) | μ1 th / eye | μ0 th / eye | ER static | ER eye | Height (mA) | Rails σ1 / σ0 | Crossing | Width (UI)
0 | 19.95 / 19.63 | 0.00 / 0.32 | ∞ | 17.86 | 17.71 | 0.27 / 0.27 | 50.0 % | 0.969
10 | 19.80 / 19.23 | 0.15 / 0.21 | 21.16 | 19.55 | 17.29 | 0.51 / 0.07 | 41.6 % | 0.969
30 | 18.62 / 17.60 | 1.34 / 0.88 | 11.44 | 13.00 | 12.37 | 0.94 / 0.50 | 19.1 % | 0.969
60 | 14.96 / 13.53 | 4.99 / 3.88 | 4.77 | 5.42 | 2.15 | 1.38 / 1.12 | 20.8 % | 0.719
Reading it
Crossing 50 → 41.6 → 19 %: the eye leans
'1' rail thickens (0.27 → 1.38 mA), '0' rail thins then thickens
μ0 below theory at 30°: the '0' swings past the null and ISI pulls it back toward it (curve folding)
Eyes computed by mzm_interconnect.eye on the reference device. Dashed: static max/min of the transfer curve (infinite bandwidth); dotted: all laser light; vertical dotted: sampling instant.

## Slide 14
3 Static phase error: mechanism
How it enters the equations
10° → 21.2 dB · 30° → 11.4 dB · 60° → 4.8 dB. The '0' sits past the null (π), so the curve folds:
Range
±180° in the GUI. Any value occurs; a bias controller nulls it continuously, so it is a demand on control range, not a performance limit. Uncontrolled beyond ~60° the eye closes.
Physical / fabrication cause
Optical path difference between the arms: width difference (Δneff), film-thickness gradient, stress, temperature gradient, DC / photorefractive drift in LiNbO3.
In INTERCONNECT
Optical Phase Shift PHS_1 (already present), phase shift = 90° + φ in radians. Wavelength-independent: a real length difference would need two waveguide elements.
EO bandwidth
Unchanged (84.47 GHz): sin Δφ0 is a flat factor (it only scales the slope).

## Slide 15
4 Vπ imbalance: effect on the eye
At a fixed 2.0 Vpp drive the swing falls short of a full Vπ,eff: eye shrinks. Re-set the drive and it is identical to balanced
d | Vπ,eff (V) | ER static @2 V | ER eye @2 V | Height @2 V | Rails σ @2 V | ER eye @Vπ,eff | Height @Vπ,eff | Chirp α
0 | 2.000 | ∞ | 17.86 | 17.71 | 0.266 | 17.86 | 17.71 | 0.000
0.05 | 2.049 | 34.56 | 17.30 | 17.40 | 0.304 | 17.86 | 17.71 | 0.024
0.2 | 2.182 | 23.67 | 15.68 | 16.56 | 0.390 | 17.86 | 17.71 | 0.091
0.5 | 2.400 | 17.61 | 13.42 | 15.30 | 0.485 | 17.86 | 17.71 | 0.200
Reading it
Fixed drive: ER 17.86 → 13.42 dB, rails 0.27 → 0.49 mA (levels leave the flat top/bottom of the cosine)
Drive = Vπ,eff: every metric equals the balanced one
What remains is chirp α = d/(2+d): visible only after fibre
Eyes computed by mzm_interconnect.eye on the reference device. Dashed: static max/min of the transfer curve (infinite bandwidth); dotted: all laser light; vertical dotted: sampling instant. Fourth eye: d = 0.5 with the drive re-set to Vπ,eff = 2.40 V.

## Slide 16
4 Vπ imbalance: mechanism
How it enters the equations
Range
±0.5 in the GUI. Typical 0.01 – 0.05. A 100 nm gap difference on a 5 µm gap is 0.02.
Physical / fabrication cause
Different overlap Γ or gap g per arm: overlay error between the waveguide and electrode masks (waveguides off-centre in the gaps), gap asymmetry, asymmetric rib over-etch changing confinement.
In INTERCONNECT
OM_1 / OM_2 (already present): phase coefficient c = −π/(VπL) and +π/(Vπ(1+d)L), L = 1 µm. Equivalently vary length.
EO bandwidth
Unchanged (84.47 GHz): g1, g2 are flat weights on the same H(f).

## Slide 17
5 Group-index imbalance: EO bandwidth and eye
The only imbalance that reshapes the frequency response. Effect grows with dn²: invisible at realistic values
dn | EO BW (GHz) | Shift | ER eye | Height | Rails σ
0 | 84.47 | +0.00 | 17.86 | 17.71 | 0.266
0.001 | 84.44 | -0.03 | 17.86 | 17.71 | 0.266
0.01 | 80.08 | -4.40 | 17.67 | 17.62 | 0.278
0.02 | 70.00 | -14.48 | 17.13 | 17.31 | 0.313
Reading it
dn = 0.001: −0.03 GHz
dn = 0.01: −4.40 GHz
Eye: slightly thicker rails from the extra ISI; ER −0.7 dB at 0.02
Eyes computed by mzm_interconnect.eye on the reference device. Dashed: static max/min of the transfer curve (infinite bandwidth); dotted: all laser light; vertical dotted: sampling instant.

## Slide 18
5 Group-index imbalance: mechanism
How it enters the equations
The ± split is symmetric, so the first-order change cancels between the arms:
Range
0 – 0.02 in the GUI (to show the mechanism). Typical below 0.001 between two arms on the same die.
Physical / fabrication cause
Different waveguide cross-section per arm: width or etch-depth difference (lithography, asymmetric over-etch), film-thickness gradient across the chip — all change the group index.
In INTERCONNECT
Two Traveling Wave Electrode elements, TW_1 → OM_1 and TW_2 → OM_2, same tables and drive; optical index = ng(1 ± dn/2).
EO bandwidth
Moves: 84.47 → 84.44 → 80.08 → 70.00 GHz for dn = 0, 0.001, 0.01, 0.02.

## Slide 19
6 Y-branch excess loss: effect on the eye
Common-mode: the whole eye shrinks toward zero by one factor. Not an imbalance, but it sets the received power
IL / branch (dB) | TY2 (theory) | μ1 (mA) | μ1 / μ1,0 | Height (mA) | ER eye | Width | Mean P (mW) | EO BW
0 | 1.000 | 19.63 | 1.000 | 17.71 | 17.86 | 0.969 | 10.00 | 84.47
0.3 | 0.871 | 17.10 | 0.871 | 15.43 | 17.86 | 0.969 | 8.71 | 84.47
1 | 0.631 | 12.39 | 0.631 | 11.18 | 17.86 | 0.969 | 6.31 | 84.47
2 | 0.398 | 7.82 | 0.398 | 7.05 | 17.86 | 0.969 | 3.98 | 84.47
Reading it
μ1 ratio equals TY2 to 3 digits
ER 17.86 dB, width, crossing: unchanged
Matters once noise is on: less signal, same noise floor → lower Q
Eyes computed by mzm_interconnect.eye on the reference device. Dashed: static max/min of the transfer curve (infinite bandwidth); dotted: all laser light; vertical dotted: sampling instant.

## Slide 20
6 Y-branch excess loss: mechanism
How it enters the equations
“Counted twice”: 0.3 dB per branch = 0.6 dB in the link.
Range
0 – 2 dB per branch in the GUI. Typical 0.1 – 0.3 dB per branch for thin-film LiNbO3, counted twice (input splitter and output combiner).
Physical / fabrication cause
Light scattered out where the waveguide divides or merges: blunt junction tip (finite lithographic resolution), mode mismatch at the branching angle, radiation in the S-bends, sidewall roughness.
In INTERCONNECT
The Y branch itself is enough: insertion loss = IL on both SPLT_1 and SPLT_2. No extra block. (The plain Optical Splitter has no such property.)
EO bandwidth
Unchanged (84.47 GHz): same fraction lost at every frequency, in both arms.

## Slide 21
Summary: effects and INTERCONNECT representation
Imbalance | Enters as | ER | Height | Width | Rails | Crossing | Mean power | EO BW | INTERCONNECT
1 Arm loss | a2 | ↓ ceiling | ↓ | — | thinner | — | ↓ | — | ATT_1: attenuation
2 Splitter | a1, a2 | ↓ ceiling | ↓ | — | thinner | — | — | — | SPLT_1: coupling coefficient
3 Static phase | Δφ0 | ↓ (folds) | ↓↓ | ↓ >60° | asymmetric | ↓ (leans) | ↓ | — | PHS_1: phase shift
4 Vπ (fixed drive) | g2 | ↓ | ↓ | — | thicker | — | — | — | OM_2: phase coefficient c
4 Vπ (drive = Vπ,eff) | g2 | — | — | — | — | — | — | — | + chirp α = d/(2+d)
5 Group index | h1, h2 | ↓ slightly | ↓ slightly | — | thicker | — | — | ↓ ∝ dn² | TW_1 / TW_2: optical index
6 Y-branch loss | TY2 | — | ↓ ×TY2 | — | ×TY2 | — | ↓ ×TY2 | — | SPLT_1, SPLT_2: insertion loss
Take-away
Five differential imbalances close or distort the eye; only the group-index one can move the EO bandwidth, and only quadratically. Y-branch loss is common-mode: it never touches ER or bandwidth, only the absolute power (and so the noise-limited Q).